## Slide 1: Concrete Durability
Henry B. Prenger, P.E.

## Slide 4: Build with Strength or Build with Durability

## Slide 5: What do we mean by Durability?
Resistance to ASR
Resistance to sulfate attack
Thermal Control in Mass Concrete
Minimizing cracking
Low permeability / Resistance to corrosion of reinforcing steel
Resistance to freeze thaw damage / Scaling

## Slide 6: U.S. Rt. 68 and MD Rt. 55
Courtesy of Maryland State Highway Administration
Notes: U.S. Route 68 over MD Rt. 55 is the highest inland bridge in Maryland. Ten years after the bridge was placed, cracking developed on the deck and the deck was replaced – with the same concrete mixture from the same ready mix company, same aggregate and cement. This was before Maryland thought they had a problem with ASR. Some testing on the Washington D.C. Metro showed deleterious ASR reaction and all aggs. In Maryland were tested as a result. The agg for this deck was found to be extremely reactive and the deck is already showing signs of deterioration.

## Slide 7
Alkali Silica Reactivity

## Slide 8
Tests | Maryland Current | Maryland 2016 | Delaware | Pennsylvania Current | Pennsylvania Future | Virginia | DC DOT | ACI 301
ASTM C1260 | ≤0.10 | ≤0.10 | <0.08** | ≤0.10 | No | No | Yes (No limit set) | No
ASTM C1567 | ≤0.10 | Case by case | <0.08** | ≤0.10 | No | No | Yes (No limit set) | ≤0.10
ASTM C1293 | No | ≤0.04 | <0.04 | No | ≤0.04 | No | No | ≤0.04
ASTM C441 | No | No | No | Yes | No | No | No | No
ASTM C295 | No | No | No | No | No | No | Yes**** | No
Mitigation |  |  |  |  |  |  |  | 
Fly Ash | (% from C1567) | (% based on aggregate reactivity) | (% based on C1567 testing** or C1293 testing***) | (% based on C1567 testing expansion ≤0.10 | 15-35% based on aggregate reactivity and type of structure | 20% (cement alkalis ≤0.75%) or 25% (cement alkalis >0.75%) | 15% maximum | % based on C1567 testing expansion ≤0.10
Slag Cement | (% from C1567) | (% based on aggregate reactivity) | (% based on C1567 testing** or C1293 testing***) | (% based on C1567 testing expansion ≤0.10 | 25-65% based on aggregate reactivity and type of structure | 40% (cement alkalis ≤0.75%) or 50% (cement alkalis >0.75%) | 50% maximum | % based on C1567 testing expansion ≤0.10
Silica fume | (% from C1567) | (% based on aggregate reactivity) | (% based on C1567 testing** or C1293 testing***) | Case by case | Calculated | 7% (cement alkalis ≤0.75%) or 10% (cement alkalis >0.75%) | No | % based on C1567 testing expansion ≤0.10
Metakaolin | No | No | No | No | No | 7% (cement alkalis ≤0.75%) or 10% (cement alkalis >0.75%) | No | Yes
Lithium | No | No | (% based on cement alkalis) | No | No | No | No | No
Low alkali cement | 0.60 | No | 0.40 | 0.60 | No | No | 0.60 | No
Alkali loading | No |  | 2.5 lbs. | No | Yes (ASTM C1778) | No | No | Yes

## Slide 9: What is Sulfate Attack?
Sulfate attack occurs when hardened concrete comes into contact with water containing sulfates. Sulfates can be found in soils, in sea water, in fertilizer and in waste water.
Sulfates react with the C3A and CaOH in cement to form and expansive material called ettringite.
Notes: Alkali Silica Reaction (ASR) is a reaction between the alkalis in portland cement and certain reactive siliceous aggregate. The reaction is fueled by water, which causes the formation an expansive gel.

## Slide 11
The reaction is more severe at locations where the concrete is exposed to wetting and drying, than continuously wet exposures.

## Slide 12: SHA Spec
Type II Cement
Type I with Fly Ash or Slag Cement with Justifying Data

## Slide 13: What is Delayed Ettringite Formation?
Concrete that undergoes high early curing temperatures form compounds that may later react in concrete, forming ettringite crystals and causing the concrete to deteriorate.

## Slide 14
DEF in a column in San Antonio, TX
Ref: FHWA/TX-08/0-4563-1

## Slide 15
 | Initial Spec | Final Spec
Concrete Temp | 70 oF | 90 oF
Temp Differential | 35 oF | Calculated
Max Temp | 135 oF | 165 oF

## Slide 16
Courtesy Swope and Associates
Concrete Footing
40’ x 35’ x 10’

## Slide 17: Woodrow Wilson Bridge
Original spec called for a max of 50% slag cement
Changed to 75% for mass concrete portions
56 day strengths specified
Strengths were exceeded at 28 days

## Slide 18
56 oF temperature differential allowed (40 oF observed)
Higher differential allowed due to reinforcing steel, increasing compressive forces due to column height

## Slide 19: SHA Spec
Evolving
Max Temperature 158 oF
Max Temperature Differential 35 oF?
Thermal Control Plan

## Slide 20: Permeability
Interstate 66 West of Washington D.C.
Notes: You see it everywhere!
I personally took this picture and it is one of many that I could use as examples.

## Slide 21: Permeability of Concrete - Corrosion
Cl -
H2O
Salty Water
Corrosion of reinforcing steel
Notes: How corrosion forms in reinforced concrete.

## Slide 22
Notes: The permeability of concrete can be measured.
ASTM C 1202 (AASHTO T277) – “Standard Test Method for Electrical Indication of Concrete’s ability to Resist Chloride Ion Penetration” otherwise known as the Rapid Chloride Permeability Test”
Basically determines the electrical conductance of concrete, providing a rapid (~20 hours after curing) indication of the resistance to the penetration of chloride ions.
This is typical data – You should always test with actual project materials before committing to a performance standard.
The permeability will decrease with age.
Ranking per ASTM C 1202
>4K = High
2-4K = Moderate
1-2K = Low
.01-1K = Very low
<.01 = Negligible

## Slide 23: SHA Spec
HPC Mix
Default due to slag cement and fly ash use

## Slide 24
Cracking

## Slide 25: Freeze Thaw Damage

## Slide 26: Inadequate Air Void System

## Slide 27
Scaling Damage

## Slide 32: Does all this matter?

## Slide 33: Concorde Overpass

## Slide 34: Lowes’ Motor Speedway Pedestrian Bridge
91 People Injured

## Slide 35: What we need to work on
20 year old spec on HPC for Bridge Decks / is it being used / should it be updated
20 year old spec for HPC for pavements
Service life for pavements
Patching Mix
ASR / a regional spec
Mass Concrete / Partnering
Scaling / Finisher certification
Cracking
Maximum chlorides in structures

## Slide 36: 90 Minutes

## Slide 38
Notes: So what can be done?
Take the day off - go fishing - think about it for awhile!
Or start designing and constructing structures that last!
This is the Confederation Bridge.
An 8-mile long bridge crossing portions of the North Atlantic Ocean to Prince Edward Island.
Under some of the harshest conditions, this bridge has a 100-year design life!!
Among design parameters, (7) different concrete mix designs were used – all of them required the incorporation of one or more Supplementary Cementitious Materials!
“Products can make the difference!!”