## Slide 1: The Concrete Industry’s Road to Quiet, Sustainable Pavement –
The Next Generation of Concrete Surfaces

## Slide 2: Introduction
John H. Roberts
Executive Director - International Grooving and Grinding Association
Vice President – American Concrete Pavement Association’s Concrete Pavement Preservation Partnership

## Slide 3: Looking Back In Time
In the not so distant past noise, ride quality and customer comfort (functional considerations) took a back seat to structural considerations.

## Slide 4: Transportation Authorities React
Transportation Authorities now place greater emphasis on tire/pavement noise, smoothness and construction delays.
  Development of tighter smoothness and new noise specifications.
  Development of low noise surface treatments.
  Increased use of sound walls.
  Night work becomes the standard.
  Safety concerns are still a priority!

## Slide 5: History Serves as Our Guide
The first concrete pavement constructed in US was located in Ohio, 1891
Used two lift construction
  Hard aggregate on surface so horseshoes wouldn’t wear pavement.
  Surface Texture was grooved in 4” squares so horses would not slip

## Slide 6: Diamond Saw Cut Surface Textures
Increasingly Specifiers are utilizing diamond saw cut surfaces to reduce roughness, reduce noise and increase the friction of their pavements, bridges, tunnels and runways.
  Economical
  Long-lasting
  Effective
  Environmentally Friendly
Evergreen Floating Bridge- Washington

## Slide 7: What Is Diamond Grinding
Removal of thin surface layer of hardened PCC using closely spaced diamond saw blades
Results in smooth, level pavement surface
Provides a longitudinal texture with desirable friction and low noise characteristics

## Slide 8: Blades and Spacers
Notes: .

## Slide 9: Typical Conventional Diamond Grinding Blade Configuration
Saw Blade
Segment
Saw Blade Core 0.105 (2.7 mm)
Spacer 0.110 (2.8 mm)
0.125
0.125 (3.2 mm )
Land Area 0.090 (2.3 mm)

## Slide 10: Diamond Grinding Equipment

## Slide 11: Conventional Diamond Ground Surface

## Slide 12: Grinding is NOT Roto Milling

## Slide 13: Milling Drums Fracture Aggregates

## Slide 14: Grinding Utilizes Abrasion Not Impact
Core
Segment
Notes: This is an individual diamond blade. The part labeled as the segment is welded onto the core. The segment holds the diamonds into the matrix. The little black specs that appear to have a trail behind them like a comment are the actual synthetic diamonds. So diamond grinding is a sawing process just like what you do with lumber. The milling uses carbide bits and is an impact process that chips away instead of saws away.

## Slide 15: Advantages of Diamond Grinding
Costs substantially less than asphalt overlays
Enhances surface friction and safety
Diamond Grinding can be accomplished during off-peak hours with short lane closures
Diamond Grinding of one lane does not require grinding of the adjacent lane
Grinding does not affect overhead clearances underneath bridges, signs or tunnels
Environmentally friendly and Sustainable

## Slide 16: Safety, Surface Texture and Friction
Increased macro-texture of diamond ground pavement surface provides for improved drainage of water at tire-pavement interface
Longitudinal texture provides directional stability and reduces hydroplaning (side-force friction). Grooves provide “escape route” for water trapped between tire and pavement surface
In Wisconsin, overall accident rates for ground surfaces were 40% less than for un-ground surfaces over a 6-year period, 57% in wet weather conditions

## Slide 17: Lower Ambient Temperatures and Energy Costs
The light reflective color of PCCP means less energy required for overhead lighting and cooling in urban areas.

## Slide 18: Pavement Surface Temperatures
Arizona State University

## Slide 19: Can be used on asphalt too!
I-70 Missouri

## Slide 20: Pavement Problems Addressed
Faulting/Roughness at joints and cracks
Built-in or construction roughness
Blends patching/surface irregularities into a consistent, identical surface
Polished concrete - Increases friction
Drainage modifications
Unacceptable noise level

## Slide 21: Joint Faulting and Roughness

## Slide 22: Grinding Removes Faults/Roughness

## Slide 23: Diamond Grinding can provide a 60% to 70% improvement over the pre-grind profile on average!
Before Grinding
After Grinding
Notes: Typical Target setup

## Slide 24: Unacceptable Noise Level

## Slide 25: Noise Performance
So, what is all this noise about tire/pavement noise?!?

## Slide 26: Transverse Tining
For many years the use of transverse tining created the perception that all concrete pavement is noisy.

## Slide 28: NCPTC OBSI Noise Testing
In 5 years the National Concrete Pavement Technology Center tested over 1500 unique textures
  Transverse Tining
  Longitudinal Tining
  Diamond Ground
  Diamond Grooved (Longitudinal, Transverse)
  Exposed Aggregate
  Pervious Concrete
  HMA and Surface treatments
Hundreds of Miles in 20 States and 6 Countries

## Slide 29: NCPTC OBSI Testing

## Slide 31: NCPTC Noise Catalogue
Research conducted by the National Concrete Pavement Technology Center shows diamond grinding as the most quiet PCCP surface texture commonly used.

## Slide 32: Caltrans & ADOT Testing

## Slide 33: Purdue-Tire Pavement Testing Apparatus
Notes: Here are a few pics of the Purdue TPAT.
The upper left shows a picture of the entire unit. It is essentially 12 foot diameter drum to which they affix curved concrete sections containing various textures. On top is a beam that rotates around the drum with instrumented tires mounted on each side of the beam. The TPTA is unique in that it allows testing of multiple surfaces under controlled laboratory conditions. This allows more efficient and precise testing without the expense of test section construction and attendant traffic control and safety issues.
The upper right photo is a pic of the DG unit built by IGGA members that allowed Purdue to impart saw cut textures on the curved concrete sections.
The lower left show a picture of the OBSI noise testing apparatus mounted near the test tire.
And the lower right pic shows the line laser used to measure macro texture.

## Slide 34: MNROAD Field Validation of TPTA
Notes: Once the NGCS surface had been verified on the Purdue TPTA, it became necessary to verify its performance on a real road when constructed with actual diamond grinding equipment. Therefore, an agency partner was necessary.
The Minnesota Department of Transportation (MnDOT) joined the effort and provided a location on their MN ROAD low volume road test track. In the summer of 2007, the IGGA funded Diamond Surfaces, Inc. to construct the Purdue NGCS surfaces at the MnROAD’s facility. The single pass and double pass NGCS surfaces were successfully constructed and verified the efficacy of the TPTA to effectively predict the noise levels of field installations1. The Purdue research indicated the NGCS should be approximately 3 dBA lower than the conventional diamond ground textures evaluated and the MN ROAD testing verified this finding.

## Slide 35: NGCS–Proof of Concept MNROAD

## Slide 36: NGCS is Built Using DG Technologies
CDG
NGCS

## Slide 37
Land area- .08 inches for hard aggregate
- .110 inches for soft aggregate
Width of diamond blades
(.125 inches)
Diamond Grinding
.75 inches
.125 inches
Saw blade thickness
(.125 inches)
Diamond Grooving
Notes: The land area for grinding differs depending on the hardness of aggregate. Grooves are more widely spaced with diamond grooving.

## Slide 38: NGCS Cross Section
.5 in .625 in
First Pass .125 in blades with .035 in spacers
Second Pass .095 in blades spaced .125 -.19 in

## Slide 39: Why Does NGCS Utilize Grooving?
Reduce the number of wet pavement accidents
The wet pavement accident occurs when the vehicle pavement friction demand exceeds the ability of the pavement-tire contact to produce the required amount of friction

## Slide 40: Improved Internal Water Drainage
Grooves provide “escape route” for water trapped between tire and pavement surface
Increases macro-texture of pavement surface.
Reduces the potential for hydroplaning

## Slide 41: What Is Hydroplaning
Hydroplaning is When Tire is Not Contacting Pavement
Notes: The figure indicates what happens during hydoplaning. When water is ponding on the surface, the faster you go the larger the wave in front of the tire. Eventually with sufficent water depth and speed, the tire literally lifts off the pavement and is skiing on the water. The operator of the vehicle at this point has no control over the vehicle.

## Slide 42: Reduced Splash and Spray
Notes: One of the benefits of Open Graded Friction Courses, in addition to their noise benefit, is their ability to prevent splash and spray. The RPA uses a TXDOT video that dramatically indicates the advantage of this type of treatment, when new, compared to an old concrete pavement. But it should be noted that the Texas ARFC has decidedly better drainage capability than the Arizona ARFC and these two surfaces should not be considered similar in performance. Under the NCAT Next Generation Study, the Arizona ARFC was tested and its permeability was stated as XX ft per day compared to more conventional OGFC surfaces which are in the range of XX to XX feet per day.
The photo above was taken on March 11, 2006 around 11:30 AM. This was the first rain after a record 143 days without rain. Notice the spray that is coming off the passenger vehicles. Not also the difference in drainability between the lane being driven in (photo taken from) and the section to the left which is not draining. Notice also the water in the wheelpaths of the lane the photo was taken from.
One of the marketing issues that needs to be considered is the strategy of comparing a new OGFC to an old concrete pavement. This is often done, but should be considered an unfair practice and should be noted. The OGFC and ARFC surfaces will change properties with time and this affects their noise qualities as well as their splash spray characteristics. This is analogous to comparing a new car to an old car.

## Slide 44: CALTANS Grooved Pavement Study
Study conducted over a four-year period
All grooved and un-grooved control sections located on freeways in urban Los Angeles County
Study includes 322 lane-miles of grooved pavement
Study includes 750 lane-miles of un-grooved control sections

## Slide 45: CALTRANS Grooving Research

## Slide 47: Mean Texture Depths – KDOT1-70
Notes: We also have a few other surfaces we are developing including NGCS Lite, which is a renewal surface texture that can be applied to existing NGCS sections in the event that friction or noise benefit is diminished over time.

## Slide 48: ASTM Locked Wheel Friction Tester

## Slide 49: Tests Conducted With 2 Tire Types
Simulates Wet Weather Conditions
Simulates dry weather conditions

## Slide 50: Kansas I-70 Test Section

## Slide 51: KDOT I-70 Noise vs. Friction
Fn Friction Number
Notes: Drive them to our website.

## Slide 52: Kansas I-70 Results
Notes: We also have a few other surfaces we are developing including NGCS Lite, which is a renewal surface texture that can be applied to existing NGCS sections in the event that friction or noise benefit is diminished over time.

## Slide 53: NCHRP Project 10-67
Notes: Drive them to our website.

## Slide 54: NGCS Site Locations in The USA

## Slide 55: International NGCS Locations
Germany
Korea
Canada
Australia

## Slide 56: South Korea - NGCS

## Slide 57: How Much Is Being Used Today? South Korea - NGCS
NGCS is used throughout South Korea on all new expressway tunnels that are 1.24 miles or more in length.
Use of the surface is now expanding to national highways and local roads as well. There are nearly 1.5 million square yards--200 lane miles--of NGCS in South Korea as of 2019.
Photo courtesy Hexacon, Inc.

## Slide 58: Case Study – I-10 Houston Texas
Known as the Katy Freeway boasting 26 lanes, it claims to be the widest roadway in the USA.
Noise sensitive area – many noise complaints from homes and businesses.
Coast to coast high intensity traffic 24 hours/day.

## Slide 59: Case Study – I-10 Houston Texas
TXDOT had considered an asphalt overlay but chose NGCS looking for a more permanent solution.
Approximately 630,000 sq. meters received the NGCS.(over 100 miles)
Average noise levels reduced by 75%
Average skid numbers increased by 60%
Smoothness improved by 73% to 305%
Texas is now the largest user of NGCS in the world.

## Slide 60: Benefits of NGCS
Smoother Ride: The innovative texture provides for a smoother, more uniform ride.
Increased Safety: Diamond grinding/grooving provide increased macro-texture, creating a safer road in wet weather conditions.
Decreased Noise: Tests have shown a decrease in tire/pavement noise by 75%.

## Slide 61: In Summary
Motorists are increasingly demanding safe, smooth, quiet and delay free roadways while funding necessary to meet these needs remains elusive.
Diamond saw-cut textures are a time proven, cost effective means of providing consistently smooth, quiet and safe textures at a competitive cost.
NGCS provides an ultra-smooth, high friction surface with acoustically durable properties, designed to last the life of the pavement.
NGCS has been constructed in 14 states and 4 countries and is THE low-noise concrete surface texture.

## Slide 62: Visit Us on the Web
International Grooving and Grinding Association
at
igga.net