## Slide 1: The Elizabeth River Tunnels Project
The Virginia Concrete Conference
Richmond, VA • March 5, 2015

## Slide 3: Mid Town Tunnel

## Slide 4: New MTT: Final Concept
Concrete shell, Immerse Tube Tunnel (ITT)
Westbound tube connecting Norfolk to Portsmouth
Two vehicular lanes and an egress corridor
Jet Fans
Deluge System
Promat
Utility Corridor
Egress Corridor

## Slide 5: ERT Project Scope
5
USA Civil Southeast Q3 Update
New, two-lane, WB tunnel
Rehab and life- safety improvements of existing MTT
Brambleton Ave. / Hampton Blvd. interchange modifications
Extending MLK to I-264, High St. interchange
Rehab and life- safety improvements of existing DTT (EB
& WB tubes)
Portsmouth
Norfolk

## Slide 12: New MTT: Element Tow Down

## Slide 13: New MTT: Elements Moored in Portsmouth

## Slide 14: New MTT: Ballast Concrete Placement

## Slide 15: New MTT: Lay Barge

## Slide 16: New MTT: Movement of Element into Slot

## Slide 17: New MTT: Element Immersion
Existing MTT Approach
New MTT Approach

## Slide 18: New MTT: Immersion of Element in Slot

## Slide 19: New MTT: Element Seals
Seals between Elements
  Gina Joint (gasket type)
  Omega Seal (inner connection)
Elements to connect to Cast in Place Approach work

## Slide 20: New MTT: Removal of Temporary Bulkheads

## Slide 21: Major Concrete Challenge / 120 Year Service Life

## Slide 26
4
Bank/Bond/TIFIA
Designers
Equity / Sponsors
Lenders
Developer
Design-Build Contractor
Operations & Maintenance
Owner
Tolling Contractor
3M

## Slide 28
Concrete Specifications

## Slide 29: Transition Here to Henry’s Thoughts for What They are Worth

## Slide 30: How do you Design for 120 Years
Look at environmental parameters (brackish water, temperatures, etc.)
Look at the geometry of the structure
Look at rebar cover
Apply a whole bunch of models (scm replacement levels, corrosion inhibitors, black steel vs. coated, etc.)
Run a ton of trial batches

## Slide 31: 120 Year Service Life (cont.)
Models Drive Concrete Towards
  Corrosion Inhibitor
Silica Fume
Low w/cm
High SCMs
Also Important
  Low Paste Content
  Cracking
70
80
90
100
110
120
130
140
150
0.32
0.34
0.36
w/cm
0.38
0.4
0.42
Time to Propagation (years)
65% Slag
70% Slag

## Slide 32: 120 Plus
Over 100 trial batches
Use fly ash for low heat, or
Change the fineness of the local slag cement, or
Use a coarser ground slag cement, and
Use blends of multiple aggregates for optimal gradation
SCC
Batching requirements tighter than C-94

## Slide 33: Agilia

## Slide 37: Concrete Mix Development
>100 Trial Batches by Lafarge for Final Mix
Optimized Aggregate Blend
Cementitious
  65% Grade 120+ Slag Cement
  35% Type I/II Portland Cement
Low Water Content
Shrinkage Reducing Admixture

## Slide 38: 14” – 20” for Inverts 16” – 22” for Doghouse

## Slide 39: 4% to 8% Air

## Slide 40: Address Differential Thermal Movement
Concrete Mix
  SRA to Reduce Autogenous Shrinkage
  Other changes Reduce the Service Life and/or Placeability
Concrete
  Precool to Reduce Max. Temperature
  Curing Compound to Reduce Drying Shrinkage
Cooling Pipes
  Reduce Temperature Rise of Concrete
Heat Existing Concrete
  Pre-Expand to Reduce Stresses
  New and Existing Cool at same Rate

## Slide 41
Addressing Restraint and Differential Thermal Movement was a Major Challenge!

## Slide 44: Pantheon – 2000 Years and Counting

## Slide 45: Air / Point of discharge, point of placement, hardened air, etc.

## Slide 46: Shrinkage

## Slide 47: Avoiding Cracks

## Slide 48: Pumping Bubblegum

## Slide 49: Mass Concrete / Slag Replacement Percentages

## Slide 50: Heat of Hydration

## Slide 51: Effect of Slag Replacement Levels on Concrete Temperatures in Mass Concrete

## Slide 52: Curing Cylinders / Match Cure and Proper Protection of Green Concrete

## Slide 53: Slag Cement Replacement Levels

## Slide 54: Curing Temperatures

## Slide 55: Concrete Color

## Slide 57: Molar Ratio

## Slide 58: Price Adjustment
902.10.10 Price Adjustment. A price adjustment will be based on the Contract unit price per cubic yard of concrete. If the unit is a lump sum item, the price per cubic yard for the concrete will be determined by dividing the cubic yards into the Contract lump sum price.

## Slide 59: US 50 and 301

## Slide 60
Aggregate Reactivity Class | Description of Aggregate Reactivity | 14 Day Expansion in C1260 | 1 Year Expansion in C1293
R0 | Non Reactive | ≤0.10 | ≤0.04
R1 | Moderately Reactive | >0.10 ≤0.30 | >0.04≤0.12
R2 | Highly Reactive | >0.30 ≤0.45 | >0.12≤0.24
R3 | Very Highly Reactive | >0.45 | >0.24
What is the science behind the classifications of the different reactivity's, R0 – R3?

## Slide 61
Size and Exposure Condition | Aggregate – Reactivity Class |  |  | 
 | R0 | R1 | R2 | R3
Non-massive concrete in a dry environment | Level 1 | Level 1 | Level 2 | Level 3
Massive elements in a dry environment | Level 1 | Level 2 | Level 3 | Level 4
All concrete exposed to humid air, buried or immersed | Level 1 | Level 3 | Level 4 | Level 5
All concrete exposed to alkalis in service | Level 1 | Level 4 | Level 5 | Level 6
Where did we come up with the levels. Is there science behind them?
Notes: Is there any science behind these levels?

## Slide 62
Significant safety, economic, or environmental consequences if minor damage
Minor risk of ASR may be acceptable
Pavements
Foundations elements
Retaining walls
Culverts
Highway barriers
Rural, low-volume roads
Precast elements in which economic costs of replacement are severe
Service life normally 40 to 74 years
Serious safety, economic, or environmental consequences if minor damage
ASR cannot be tolerated
Major bridges
Power plants
Dams
Nuclear facilities
Water treatment facilities Waste water treatment facilities Tunnels
Critical elements that are very difficult to inspect or repair
Service life normally more than 75 years
SC3
SC4
Is there science behind the service life predictions?

## Slide 63: Size Doesn’t Matter

## Slide 64: Cubes for Grout??????????????

## Slide 65: Measuring Permeability